## Slide 1
Ultra-Fast Silicon Detector
The “4D” challenge
A parameterization of time resolution
The “Low Gain Avalanche Detectors” project
Laboratory measurements
UFSD: LGAD optimized for timing measurements
WeightField2: a simulation program to optimize UFSD
First measurements
Future directions
Nicolo Cartiglia
With
INFN Gruppo V, LGAD group of RD50, FBK and Trento University, Micro-Electronics Turin group
Rome2 - INFN.

## Slide 2
This work is currently supported by INFN Gruppo V, UFSD project (Torino, Trento Univ., Roma2, Bologna, FBK).
This work was developed in the framework of the CERN RD50 collaboration and partially financed by the Spanish Ministry of Education and Science through the Particle Physics National Program (F P A2010−22060−C 02−02 and FPA2010 − 22163 − C02 − 02).
The work at SCIPP was partially supported by the United States Department of Energy, grant DE-FG02-04ER41286.
Acknowledgement
This research was carried out with the contribution of the Ministero degli Affari Esteri, “Direzione Generale per la Promozione del Sistema Paese” of Italy.
Notes: 2

## Slide 3
The 4D challenge
Is it possible to build a detector with concurrent excellent time and position resolution?
Can we provide in the same detector and readout chain:
Ultra-fast timing resolution [ ~ 10 ps]
Precision location information [10’s of mm]

## Slide 4
State-of-the-art Timing Detectors
Timing detectors exploit very fast physics processes such as
Cherenkov light emission or electronic avalanches to create prompt signals
CMS/ATLAS
ALICE
These detectors measure time very accurately but locate particles with the precision of ~ 1 mm
Good timing is obtain by using a gain mechanism, either in the detector or in the electronics
st ~ 20-30 ps
sx ~ 1-2 mm

## Slide 5
State-of-the-art Position Detectors
Extremely good position detectors are currently in use in every major high energy physics experiment:
Millions of channels
Very reliable
Very radiation hard
The timing capability is however
limited to ~ 100-150 ps
(NA62 @CERN)
st ~ 100-150 ps
sx ~ 20-30 mm

## Slide 6
A time-tagging detector
The timing capabilities are determined by the characteristics of the signal at the output of the pre-Amplifier and by the TDC binning.
Time is set when the signal crosses the comparator threshold
(a simplified view)

## Slide 7
Noise source: Time walk and Time jitter
Time walk: the voltage value Vth is reached at different times by signals of different amplitude
Jitter: the noise is summed to the signal, causing amplitude variations
Due to the physics of signal formation
Mostly due to electronic noise
sTotal2 = sJitter 2 + s Time Walk 2 + sTDC2

## Slide 8
Time Resolution and slew rate
Assuming constant noise, to minimize time resolution
we need to maximize the S/tr term
(i.e. the slew rate dV/dt of the signal)
 We need large and short signals 
where:
- S/tr = dV/dt = slew rate
- N = system noise
- Vth = 10 N
Using the expressions in the previous page, we can write
Notes: 8

## Slide 9
Signal formation in silicon detectors
We know we need a large signal, but how is the signal formed?
A particle creates charges, then:
The charges start moving under the influence of an external field
The motion of the charges induces a current on the electrodes
The signal ends when the charges reach the electrodes
What is controlling
the slew rate?

## Slide 10
How to make a good signal
Signal shape is determined by Ramo’s Theorem:
Drift velocity
Weighting field
A key to good timing is the uniformity of signals:
Drift velocity and Weighting field need to be as uniform as possible

## Slide 11
Drift Velocity
 Highest possible E field to saturate velocity
 Highest possible resistivity for velocity uniformity
We want to operate in this regime

## Slide 12
Weighting Field: coupling the charge to the electrode
The weighting field needs to be as uniform as possible, so that the coupling is always the same, regardless of the position of the charge
Strip: 100 mm pitch, 40 mm width
Pixel: 300 mm pitch, 290 mm width
Bad: almost no coupling away from the electrode
Good: strong coupling almost all the way to the backplane

## Slide 13
Non-Uniform Energy deposition
Landau Fluctuations cause two major effects:
Amplitude variations, that can be corrected with time walk compensation
For a given amplitude, the charge deposition is non uniform.
These are 3 examples of this effect:

## Slide 14: What is the signal of one e/h pair?
However the shape of the signal depends on the thickness d:
thinner detectors have higher slew rate
D
+
-
d
+
-
(Simplified model for pad detectors)
Let’s consider one single electron-hole pair.
The integral of their currents is equal to the electric charge, q:
i(t)
t
Thin detector
Thick detector
One e/h pair generates higher current in thin detectors
Weighting field

## Slide 15: Large signals from thick detectors?
The initial current for a silicon detector does not depend on how thick (d) the sensor is:
Number of e/h = 75/micron
Weighting field
velocity
Initial current = constant
(Simplified model for pad detectors)
D
d
+
-
+
-
+
-
+
-
+
-
+
-
+
-
Thick detectors have higher number of charges:
However each charge contributes to the initial current as:

## Slide 16: Thin vs Thick detectors
(Simplified model for pad detectors)
D
d
+
-
+
-
+
-
+
-
+
-
+
-
+
-
Thick detectors have longer signals, not higher signals
i(t)
Thin detector
Thick detector
S
tr
How can we do better?
Best result : NA62, 150 ps on a 300 x 300 micron pixels

## Slide 17
Possible approaches
We need to minimize this expression:
  APD (silicon with gain ~ 100): maximize S
    Very large signal
  Diamond: minimize N, minimize tr
    Large energy gap, very low noise, low capacitance
    Very good mobility, short collection time tr
  LGAD (silicon with gain ~ 10): minimize N, moderate S
    Low gain to avoid shot noise and excess noise factor
Notes: 17

## Slide 18
The APD approach
The key to this approach is the large signal: if your signal is large enough, everything becomes easy.
So far they reported:
Excellent time resolution
Good radiation resistance up to < 1014 neq/cm2
They will propose a system for the CT-PPS
See:
https://indico.cern.ch/event/363665/contribution/7/material/slides/0.pdf

## Slide 19
The Diamond approach - I
Diamond detectors have small signal: two ways of fighting this problem
1) Multilayer stack
2) Grazing
The signal is increased by the sum of many layers while it keeps very short rise time
The particle crosses the diamond sensor along the longitudinal direction
Best resolution:
~ 100 ps

## Slide 20
The Diamond approach - II
TOTEM collaboration: couple diamond detector with a tailored front-end and a full digitizing readout (SAMPIC, Switching Capacitor Sampler)
Excellent results at a very recent testbeam with ~ 4.5 x 4.5 mm2 detectors
The result allows TOTEM to introduce timing measurement is their Roman Pot set-up:
Vertical top pots used for timing

## Slide 21
The “Low-Gain Avalanche Detector” approach
Is it possible to manufacture a silicon detector that looks like a normal pixel or strip sensor, but with a much larger signal (RD50)?
750 e/h pair per micron instead of 75 e/h?
Finely Segmented
Radiation hard
No dead time
Very low noise (low shot noise)
No cross talk
Insensitive to single, low-energy photon
Many applications:
Low material budget (signal in 30 micron == signal 300 micron)
Excellent immunity to charge trapping (larger signal, shorter drift path)
Very good S/N: 5-10 times better than current detectors
Good timing capability (large signal, short drift time)

## Slide 22
Gain in Silicon detectors
Gain in silicon detectors is commonly achieved in several types of sensors. It’s based on the avalanche mechanism that starts in high electric fields: E ~ 300 kV/cm
Silicon devices with gain:
APD: gain 50-500
SiPM: gain ~ 104
Charge multiplication
Gain:
= strong E dependance
~ 0.7 pair/μm for electrons,
~ 0.1 for holes
-
-
-
+
-
-
+
-
-
+
+
+
-
-
-
+
-
-
+
-
-
+
-
-
+
+
+
-
+
+
-
E ~ 300 kV/cm
Concurrent multiplication of electrons and holes generate very high gain

## Slide 23
How can we achieve E ~ 300kV/cm?
1) Use external bias: assuming a 300 micron silicon detector, we need Vbias = 30 kV
E = 300 kV/cm  q ~ 1016 /cm3
2) Use Gauss Theorem:
30 kV !!
Not possible

## Slide 24
Low Gain Avalanche Detectors (LGADs)
The LGAD sensors, as proposed and manufactured by CNM
(National Center for Micro-electronics, Barcelona):
High field obtained by adding an extra doping layer
E ~ 300 kV/cm, closed to breakdown voltage
Gain layer
High field

## Slide 25
LGADs Pads, Pixels and Strips
The LGAD approach can be extended to any silicon structure,
not just pads.
This is an example of LGAD strips

## Slide 26
Sensor: Simulation
We developed a full sensor simulation to optimize the sensor design
WeightField2, F. Cenna, N. Cartiglia 9th Trento workshop, Genova 2014
Available at http://personalpages.to.infn.it/~cartigli/weightfield2
It includes:
Custom Geometry
Calculation of drift field and weighting field
Currents signal via Ramo’s Theorem
Gain
Diffusion
Temperature effect
Non-uniformdeposition
Electronics

## Slide 27
WeightField2: a program to simulate silicon detectors

## Slide 28
WeightField2: output currents

## Slide 29
WeightField2: response of the read-out electronics

## Slide 30
How gain shapes the signal
+
-
+
+
-
-
Gain electron: absorbed immediately
Gain holes:
long drift home
Initial electron, holes
Electrons multiply and produce additional electrons and holes.
Gain electrons have almost no effect
Gain holes dominate the signal
 No holes multiplications

## Slide 31: Interplay of gain and detector thickness
The rate of particles produced by the gain does not depend on d (assuming saturated velocity vsat)
Particles per micron
Gain
+
-
v
Gain
 Constant rate of production
 Gain current ~ 1/d
However the initial value of the gain current depends on d
(via the weighing field)
A given value of gain has much more effect on thin detectors

## Slide 32: Gain current vs Initial current
!!!
 Go thin!!
(Real life is a bit more complicated, but the conclusions are the same)
300 micron:
~ 2-3 improvement with gain = 20
Full simulation
(assuming 2 pF detector capacitance)
Significant improvements in time resolution require thin detectors

## Slide 33
Ultra Fast Silicon Detectors
UFSD are LGAD detectors optimized to achieve the best possible time resolution
Specifically:
Thin to maximize the slew rate (dV/dt)
Parallel plate – like geometries (pixels..) for most uniform weighting field
High electric field to maximize the drift velocity
Highest possible resistivity to have uniform E field
Small size to keep the capacitance low
Small volumes to keep the leakage current low (shot noise)

## Slide 34
First Measurements and future plans
LGAD laboratory measurements
Doping concentration
Gain
Time resolution measured with laser signals
LGAD Testbeam measurements
Landau shape at different gains
Time resolution measured with MIPs

## Slide 35
LGAD Sensors in Torino
DR
DC
Run | Sensor | P-Layer Implant (E=100 KeV) | Gain | Vbreak | Metal Layer
6474 | W8_B4 | ? | ~ 10 | > 500 V | DR
6474 | W8_C6 | ? | ~ 10 | > 500 V | DC
6474 | W9_B6 | No implant | No Gain | > 500 V | DR
7062 | W1_F3 | 1.6 x 1013 cm-2 | ~ 1-2 | > 500 V | DR
7062 | W3_H5 | 2.0 x 1013 cm-2 | ~ 10 | > 500 V | DR
7062 | W7_D7 | No implant | No Gain | > 500 V | DR
Thickness:
300 μm

## Slide 36
Doping profile from CV measurement - I
Doping
No-gain sensor
Doping profile

## Slide 37
Doping profile from CV measurement - II
Gain sensor
Ideal doping profile
Doping profile
This “bump” creates the high field needed for the gain

## Slide 38
Signal amplitude
Reference sensor
Gain ~ 10
Using laser signals we are able to measure the different responses of LGAD and traditional sensors

## Slide 39
Digitizer
2 sensors
Laser split into 2
Gain
Gain ~ 10
The gain is estimated as the ratio of the output signals of LGAD detectors to that of traditional one
Gain ~ 20
The gain increases linearly with Vbias (not exponentially!)

## Slide 40: Laser Measurements on CNM LGAD
We use a 1064 nm picosecond laser to emulate the signal of a MIP particle (without Landau Fluctuations)
The signal output is read out by either a Charge sensitive amplifier or a Current Amplifier (Cividec)
st ~ 140 ps @ 800 Volts

## Slide 41: Testbeam Measurements on CNM LGAD
In collaboration with Roma2, we went to Frascati for a testbeam using 500 MeV electrons
300 micron thick, 5 x5 mm pads
The gain mechanism preserves the Landau amplitude distribution of the output signals
As measured in the lab, the gain ~ doubles going from 400 -> 800 Volt.

## Slide 42: 100 GeV pion Testbeam with CNM LGAD
Teasbeam data understood as the sum of 1MIP, 2 MIP or 3 MIP
300 micron thick, 5 x5 mm pads
Very linear behavior of UFSD with increasing charge

## Slide 43: Properties of the Landau distributions
Chart: 
| 600.0 | 800.0 | 1000.0
Sigma/MPV | 0.098561 | 0.10419 | 0.097466
The ratio sigma/MPV is constant as a function of multiplication
indicating that the excess noise factor is not playing a role yet
Pulse Height Dispersion
DA/A = 0.7079d-0.266
According to our fits, the Landau have a smaller width than what is proposed by the parameterization of Meroli et al.
Sigma/MPV
Sigma/MPV

## Slide 44: Testbeam Measurements on CNM LGAD
Time difference between two LGAD detectors crossed by a MIP
st ~ 190 ps @ 800 Volts
Tested different types of electronics (Rome2 SiGe, Cividec),
Not yet optimized for these detectors

## Slide 45: Present results and future productions
With WF2, we can reproduce very well the laser and testbeam results.
Assuming the same electronics, and 1 mm2 LGAD pad with gain 10, we can predict the timing capabilities of the next sets of sensors.
Current Test beam results and simulations
Next prototypes
Effect of
Landau
fluctuations

## Slide 46: Effect of Landau Fluctuations on the time resolution
The effect of Landau fluctuations in a MIP signal are degrading the time resolution by roughly 30 % with respect of a laser signal
Current Test beam results and simulations
Next prototypes

## Slide 47
Digitizer
Irradiation tests
The gain decreases with irradiations:
at 1014 n/cm2 is 20% lower
 Due to boron disappearance
What-to-do next:
1) Planned new irradiation runs (neutrons, protons), new sensor geometries
2) Use Gallium instead of Boron for gain layer (in production now)
3) Design the UFSD to have a gain higher than we need, ~ 30 at 500 V.
- We use UFSD at gain 10-15, at 200 Volt
- When radiation damage lowers the gain, we increase Vbias to compensate

## Slide 48: Merging timing with position resolution
Electrode segmentation makes the E field very non uniform, and therefore ruins the timing properties of the sensor
We need to find a geometry that has very uniform E field, while allowing electrode segmentation.

## Slide 49: 1) Segmentation: buried junction
Separate the multiplication side from the segmentation side
Moving the junction on the deep side allows having a very uniform multiplication, regardless of the electrode segmentation
n-in-p
p-in-p
Move the gain layer to the deep side
For a 100 mm detector, the current does not change
Parallel plate geometry
Segmented geometry

## Slide 50: 2) Segmentation: AC coupling
gain layer
AC coupling
Standard n-in-p LGAD, with AC read-out
n+ electrode
Detector
Detector
Detector
Detector
Detector
Detector
AC coupling
The signal is frozen on the resistive sheet, and it’s AC coupled to the electronics
p++ electrode

## Slide 51: 3) Segmentation: splitting gain and position measurements
The ultimate time resolution will be obtained with a custom ASIC. However we might split the position and the time measurements

## Slide 52: Electronics
Pads with gain
Current due to gain holes creates a longer and higher signal
2 sensors
Pads with no gain
Charges generated uniquely by the incident particle
Simulated Weightfield2
Oscilloscope
Gain
Initial
300 mm
300 mm
To fully exploit UFSDs, dedicated electronics needs to be designed.
The signal from UFSDs is different from that of traditional sensors

## Slide 53: Interplay of TCol and t = Rin CDet
Detector Capacitance CDet
Input impedance Rin
There are two time constants at play:
TCol : the signal collection time (or equivalently the rise time)
t = Rin CDet : the time needed for the charge to move to the electronics
Collection
time TCol
Rin CDet
t < TCol
t/TCol increases  dV/dt decreases
 Smoother current
Electronics
Signal
Need to find the optimum balance
t ~ TCol
t > TCol

## Slide 54: What is the best “time measuring” circuit?
10%
t1 t2
Constant Fraction Discriminator
The time is set when a fixed fraction of the amplitude is reached
Time over Threshold
The amount of time over the threshold is used to correct for time walk
Multiple sampling
Most accurate method, needs a lot of computing power: SAMPIC!!
Vth
t
t
t
V
V
V

## Slide 55
Laser split into 2
Noise - I
Detector Bias
Bias Resistor
Detector Cdet
CBias
RBias
CC
RS
Digitizer
2 sensors
CDet
RBias
RS
iN_Det
iN_Amp
eN_Amp
eN_S
iN_Bias
Detector
Bias
Resistor
Series
Resistor
Amplifier
Real life
Noise Model
This term, the detector current shot noise, depends on the gain
This term dominates for short shaping time
low gain!

## Slide 56
Laser split into 2
Noise - II
Detector Bias
Bias Resistor
Detector Cdet
CBias
RBias
CC
RS
Real life
k = ratio h/e gain
NOISE DUE TO GAIN:
Excess noise factor:
low gain, very small k
Low leakage current and low gain (~ 10) together with short shaping time are necessary to keep the noise down.

## Slide 57
Next CNM productions
5 mm
2.5 mm
1.25 mm
0.6 mm
Timescale:
Spring 2015: 200 micron
Summer 2015: 100 micron
Summer 2015: 50 micron
These new productions will allow a detailed exploration of the UFSD timing capabilities, including border effects between pads, and distance from the sensor edge.

## Slide 58: Next Steps
Wafer Production
    200 micron thick sensors by Spring-2015
    100 and 50 micron thick sensors by Summer 2015.
Production of UFSD doped with Gallium instead of Boron.
Study of reversed-UFSD started for the production of pixelated UFSD sensors (FBK, Trento).
UFSD are included in the CMS TDR CT-PPS as a solution for forward proton tagging
Use of UFSD in beam monitoring for hadron beam. INFN patent and work on-going
Interest in UFSD for 4D tracking at high luminosity
Testbeam analyses just started. Results coming soon…

## Slide 59
UFSD – Summary
We are just starting to understand the timing capability of UFSD
Low-gain avalanche diodes (LGAD) offer silicon sensors with an enhanced signal amplitude: UFSD are LGAD detectors optimized for timing resolution.
Several options under studies to obtain concurrently excellent space and time resolutions.
We developed a program, Weightfield2 to simulate the behaviors of LGAD and optimized them for fast timing (available at http://personalpages.to.infn.it/~cartigli/Weightfield2.0/)
Timescale: 1 year to asses UFSD timing capabilities

## Slide 60
Presented at IEEE, oral and posters, presentations
Poster Session IEEE N11-8
Poster Session IEEE N26-13

## Slide 61
Additional references
Several talks at the 22nd, 23rd and 24th RD50 Workshops:
23rd RD50: https://indico.cern.ch/event/265941/other-view?view=standard
22nd RD50: http://panda.unm.edu/RD50_Workshop/
9Th Trento Workshop, Genova, Feb 2014.
F. Cenna “Simulation of Ultra-Fast Silicon Detectors”
N. Cartiglia “Timing capabilities of Ultra-Fast Silicon Detector”
Papers:
[1] N. Cartiglia, Ultra-Fast Silicon Detector, 13th Topical Seminar on Innovative Particle and Radiation Detectors (IPRD13), 2014 JINST 9 C02001, http://arxiv.org/abs/1312.1080
[2] H.F.-W. Sadrozinski, N. Cartiglia et al., Sensors for ultra-fast silicon detectors, Proceedings "Hiroshima" Symposium HSTD9, DOI: 10.1016/j.nima.2014.05.006 (2014).

## Slide 62
Backup

## Slide 63
The “Low-Gain Avalanche Detector” project
Is it possible to manufacture a silicon detector that looks like a normal pixel or strip sensor, but
with a much larger signal (RD50)?
Poster Session IEEE N26-13
730 e/h pair per micron instead of 73 e/h
Finely segmented
Radiation hard
No dead time
Very low noise (low shot noise)
No cross talk

## Slide 64
How can we progress? Need simulation
We developed a full simulation program to optimize the
sensor design, WeightField2, (http://cern.ch/weightfield2 )
It includes:
Custom Geometry
Calculation of drift field and weighting field
Currents signal via Ramo’s Theorem
Gain
Diffusion
Temperature effect
Non-uniform deposition
Electronics
Poster Session IEEE N11-8

## Slide 65
State-of-the-art Position Detectors
Extremely good position detectors are currently in use in every major high energy physics experiment:
Millions of channels
Very reliable
Very radiation hard
The timing capability is however
limited to ~ 100-150 ps
(NA62 @CERN)
st ~ 100-150 ps
sx ~ 20-30 mm

## Slide 66
Why low gain? Can we use APD or SiPM instead?
My personal conclusion: I think it’s possible to obtain very good timing: APDs, SiPMs have very high gain, so they are excellent in “single shot” timing.
However, we are seeking to obtain something more powerful: a very low noise, finely pixelated device, able to provide excellent timing in any geometry, and also able to work in the presence of many low energy photons without giving fake hits.
These requirements make the use of high gain devices challenging

## Slide 67
Comparison Data Simulation
MIP
Alpha from Top
Alpha from bottom
V bias
200
300
400
500
600

## Slide 68
CNM LGADs mask
Wafer Number | P-layer Implant (E = 100 keV) | Substrate features | Expected Gain
1-2 | 1.6 × 1013 cm-2 | HRP 300 (FZ; ρ>10 KΩ·cm; <100>; T = 300±10 µm) | 2 – 3
3-4 | 2.0 × 1013 cm-2 | HRP 300 (FZ; ρ>10 KΩ·cm; <100>; T = 300±10 µm) | 8 – 10
5-6 | 2.2 × 1013 cm-2 | HRP 300 (FZ; ρ>10 KΩ·cm; <100>; T = 300±10 µm) | 15
7 | (---) PiN Wafer | HRP 300 (FZ; ρ>10 KΩ·cm; <100>; T = 300±10 µm) | No Gain
CNM, within the RD50 project, manufactured several runs of LGAD, trying a large variety of geometries and designs
This implant controls the value of the gain

## Slide 69: Electronics: What is the best pre-amp choice?
Current Amplifier
Integrating Amplifier
Current signal in a 50 mm sensor
Energy deposition in a 50 mm sensor
Fast slew rate
Higher noise
Sensitive to Landau bumps
Slower slew rate
Quieter
Integration helps the signal smoothing

## Slide 70: Details of AC coupling - I
Detector
Detector
Detector
Detector
Detector
Detector
C AC
RAmpl
RSheet
Additional Rise time ~ RAmpl * Cdetector ~ 100 W * 1pF ~ 100 ps
Freezing time ~ RSheet * CAC ~ 1kW * 100pF ~ 100 ns
Only a small part of the detector is involved

## Slide 71: Details of AC coupling - II
gain layer p+
AC coupling
n++ electrode
In the n-in-p design, the resistivity of the sheet is hard to control, as the doping of the n++ and p+ layers determine the gain, so the values cannot be chosen as we like.
Gain layer p+
AC coupling
n++ electrode
In the p-in-p design, the resistivity of the sheet is easier to control
p++ electrode
p++ electrode