## Slide 1: French-Ukraine workshop – LAL
French Task force for Phase 2 ATLAS Tracker construction
Giovanni Calderini – LPNHE, Paris
Abdenour Lounis- LAL, Orsay
Future Contributions of LPNHE & LAL
and IRFU

## Slide 2: Overview of the presentation
Introduction to the ATLAS context
Contributions to the development of the Inner Tracker system
Future plans for ATLAS ITK construction
Infrastructures to contribute as an ATLAS pixel production center
Conclusions

## Slide 3: Pixel sensors R&D groups (Almost 10 yea rs)- People involved
LPNHE:
G. Calderini
M. Bomben, G. Marchiori, F. Cresoli,
PhD student : A. Ducourthial , J. Chauveau
Yourii Piadyk, Mykyta Haranko (Kiev)
LAL:
A. Lounis,
Phd Students : T. Rashid+ Dmytro Hohov (Kiev)
Past contributions: C. Nellist (PostDoc), E. Gkougkousis (PhD)
A. Bassalat (PhD), M. Benoit (PhD), J. Idarraga (PostDoc), Vladimir Linhard (PostDoc)
For the Construction: D. Varouchas, L. Fayard, C.A. Bourdarios, R.Tanaka

## Slide 4: ATLAS detector
Huge multi-purpose detector; 46 m long; diameter 22 m; weight 7000 t
Tracking system: 7 m long; diameter 2.3 m; 2 T field

## Slide 5: ATLAS Tracker at LHC
Large Hadron Collider in ~27km, E=14 TeV, L=1034 cm-2s- Beam-crossing: 40MHz
    1 GHz interaction rate, 103 particles each 25 ns.
Tracking detectors must fulfill the conditions:
    Fast (40MHz), Rad-Hard (10-100kGy), high granularity & good pattern recognition capabilities (103 tracks/25 ns).
Environment is very radiation hostile: Accuracy and we should be able to measure tracks!
    To measure momenta (dynamics, invariant masses)
    To measure vertices
        Primary  improve on p and E measurements
        Secondary  tag ps living particles (b,t) markers of events with significant physics content
    To help identifying photons

## Slide 6
Bref summary of what has been acheived

## Slide 7: Focus on the actual pixel system
Existing B-layer
Newbeam pipe
IBL mounted on beam pipe
Actual geometry
NEW LAYER ADDED IBL 30 mm radius

## Slide 8: Past important contributions
IN2P3 important contributions
(2010-2015) for the Insertable B Layer project :
  Sensors
  Cooling
  Mechanics
  Integration
  Work in Labs & manpower
  (1 LAL-PhD student @CERN)

## Slide 9: One important issue at LHC: Extreme radiation levels !
Plots show radiation dose and fluence per high luminosity LHC year for ATLAS (assuming 107 s of collisions; source: ATL-Gen-2005-001)
Fluence [1 MeV eq. neutrons/cm2] Radiation dose [Gray/year]
“Uniform thermal neutron gas” Put your cell phone into ATLAS !
It stops working after 1 s to 1 min.
Neutrons are everywhere and cannot easily be suppressed

## Slide 10: Radiation-hard sensors
Radiation induced leakage current
independent of impurities; every 7C
of temperature reduction halves current
cool sensors to  -25C (SCT = -7C)
“type inversion” from n to p-bulk
 increased depletion voltage
oxygenated silicon helps (for protons);
n+-in-n-bulk or n+-in-p-bulk helps
Charge trapping
the most dangerous effect at high fluences
 collect electrons rather than holes
 reduce drift distances
Notes: Expand this into a few slides

## Slide 11: Alternatives for Planar pixel technology
n+
p+
n- bulk
Al
SiO2
Guard Ring
Bias Ring
p-spray/stop
Guard Ring
Bias Ring
n-in-n
n-in-n
More expensive
Double-sided processing
Limited suppliers
Some experience with “large” scale production
  CMS/ATLAS pixels, LHCb VELO
n+
p+
p- bulk
Al
SiO2
Guard Ring
Bias Ring
p-spray/stop
n-in-p
n-in-p
~50% less expensive than n-in-n
Single-sided processing
More suppliers (Japan, EU )
Limited production experience
Better radiation hard tolerance
n+ R/O kept
Present
Future

## Slide 12: Pixel Module Detection Unit
Intrinsic Module Detection device
Silicon sensor
Readout chip
Bump bond connection
Hybrid pixel detector:
The sensor and the readout electronic are realized in different semiconductor substrates
Size of the electronic readout pixels is equal to the size of the sensor pixels
The connection between the electronic and the sensor is done via bump bond connections
Bias plane
Pixe Matrix

## Slide 13: R&D :Towards (n-in-p) Edgless Sensors for the future
ATLAS pixel detector uses n-in-n-sensors
  double sided processing (back side is structured)
  all sensor edges at ground
  most expensive part of the module
  Exploring n-in-p sensors as alternative
  Studies show radiation hardness (LAL&LPNHE Member of RD50 coll.)
  single sided process ~ price benefit of factor 2-3
    Develop Active Edge Technology
  Absence of guard rings on back side lead to risk of (destructive) sparking to the ROC
n-in-n
n-in-p

## Slide 14: LPNHE & LAL: Active contributions within ATLAS Pixel R&D
  Tasks to improve the Planar Pixel Silicon detector for the ATLAS upgrade
  Goals
  Performance : evaluate & improve sensor design for radiation tolerance up to 3x1015neq/cm2 fluence.
  Productions : work on various wafer productions (Cis, VTT Advacam & FBK)
Simulation
Doping concentration
Charge collection
n+
Bias-rail
Poly-Si
P-stop
Bump
e-
e-
e-
h
h
h
Guard Ring
Under Bump
Metalization
Active Edge
Smaller Edge size
Higher Efficiency at Edge region
Biasing Structure
Optimize Biasing structure
Higher Efficiency at Pixel boundary
Bumpbonding
Better UBM material
Higher Flip-Chip Yield
Radiation Tolerance
Assembly
Production…

## Slide 15: DUT#20 DUT#21
Edgless & Slim edge Pixels for Phase 2
Typical pixel sensor design for phase 2
  n-in-p common ATLAS wafer production VTT- ADVACAM- Finlande
  Characterized in clean room at LAL and tested in Beam tests at CERN
ADVACAM NP100-7-2A
(thickness – 100 um) slim edge
ADVACAM NP150-6-1A
(thickness – 150 um) active edge design
100 um
50 um
Guard Ring
Bias Ring
Punch-through structure

## Slide 16: Hit-efficiency at the edge
Hit-efficiency above 90% up to 40 µm away from the last pixel
No good tracks beyond -50 µm due to quality cuts

## Slide 17
Efficiencies from beam tests
- Efficiency vs track impact position DUT#22
Pixel border
Sensor border
Last pixel column
(250 um)
Analysis from Dmytro Hohov ATLAS@LAL

## Slide 18: Irradiated pixel behavior at high fluence
Pixel Matrix Hitmap at 5. 1015 neq/cm2 and Temperature -150c.
Beam-tests results
Position of polarization rail
O0tilt
150 tilt
Loss of Effiicency around Bias rails and implants
Eudet 120 GeV pions/ F=4x1015 neq cm-2
Bias Rail

## Slide 19
Future plans for ATLAS ITK construction

## Slide 20: Roadmap for ATLAS phase 2
Installation IBL
Fast track (FTK) for Trigger
Trigger upgrade
Full replacement
Replacement of Front-End electronics
Forward Calorimeter upgrade.
Front end Electronics replacement
Tile calorimeter
Argon liquid Calorimeter (LAr)
Internal Detector
<m> =
140-200
<m> =
50-80
Muon spectrometer
LUMINOSIY

## Slide 21: Challenges for a new inner tracker
But !
Same or better performance required !
  Use quite “transparent tracker” Low X0
  Provide V. High granularity sensors
  Go du deep submicron technologies
  Raise the transfer data band-with (5Gps)
  Improve the layout and mechanics
High Luminosity LHC conditions will affect
Drastically the current design
Peak Luminosity will increase by a factor 5-7 :
5-7 10**34
Average Pileup : a factor of 8 <m> ~200
Integrated luminosity : a factor 10 : 3000 fb-1
Radiation hardness : a factor 20 : 2x10 neq/cm2

## Slide 22: Expected fluences (1 MeV neq.cm-2)
ATLAS ITk Simulation, FLUKA to 3,000 fb-1
8 MGy , 1.4x1016 n cm-2
1 MGy , 2x1015 n cm-2
2 MGy , 4x1015 n cm-2
L0
L0
L1
Pixels | R (mm) | Fluence Max (Neq/cm2) | Dose (Mrad)
Layer 0 | 39 | 2,25 .10*16 | 1710
Layer 1 | 75 | 0,82 .10*16 | 715
Layer 2 | 155 | 0,25 .10*16 | 148
Layer 3 | 213 | 0,12 .10*16 | 96
Layer 4 | 271 | 0,12 .10*16 | 61
Endcap | 80 | 0,67 .10*16 | 687

## Slide 23: Production planning of the next Pixel Tracker : Planning 2017-2025
2017
Q1 | Q2 | Q3 | Q4
Q1 | Q2 | Q3 | Q4
Q1 | Q2 | Q3 | Q4
Q1 | Q2 | Q3 | Q4
Q1 | Q2 | Q3 | Q4
Q1 | Q2 | Q3 | Q4
Q1 | Q2 | Q3 | Q4
Q1 | Q2 | Q3 | Q4
Q1 | Q2 | Q3 | Q4
2018
2019
2020
2025
2021
2022
2023
2024
Estimation for the module production including the loading
32-36 months
RD53-A test
FE design
Pre-prod
Pre-prod
PIT
Test in SR1
Integration
Module production
Loading
CERN
Production centers
sensors

## Slide 24: Estimation in terms of module construction
Fully inclined (Front-end) | 
Layer 0 | 936 FE
Layer 1 | 2016 FE
Layer 2 | 3200 FE
Layer 3 | 4752 FE
Layer 4 | 6264 FE
Rings | 
Layer 0 | 3264 FE
Layer 1 | 5472 FE
Layer 2 | 6144 FE
Layer 3 | 7680 FE
Total | 22560 FE
Total | 17168 FE
Contribution (LAL+ LPNHE)~ ~1000-2000 Modules
Supposing single chip for layer 0
double chip module Layer 1
Quads for Layers 3 et 4
Total Modules including rings ~ 12.000 Modules
Quad
singlet
doublet
Quad FEI4 Module prototype
Major investment of IN2P3 for ITK
LAL-IN2P3-CPPM-LPSCG-LAPP

## Slide 25
DEBUG
Probe tests
connexion
Module construction
RECEPTION-INSPECTION OPTICAL TESTS ONE WAFER SI -SENSORS INDIVIDUAL TESTING OR WAFER TESTINGS
INTERCONNECTION MATRICES PIXELS WITH INDIUM BUMPS / PIXEL SENSORS TO READOUT CHIP (FLIP-CHIP)
CONNECTION OF MODULE ON READOUT CARD (WIRE BOND)
Wire bonding
GLUING OF FLEX CABLE AND WIRE BONDS OF SIGNAL, BIAS, TENSION, CLOCKS
COMPLETE CHARACTERIZATION AND MODULE SELECTION ACCORDING TO GRADES ,DATABASE Classification
EXPEDITION OF MODULES SELECTED TOWARS LOADING AND INTEGRATION CENTERS (CERN, CPPM, et…..)
Tests on modules with béta source , laser …
NO
OK
SITE : : LAL LPNHE
LAL LPNHE
LAL LPNHE+ IRFU
INDUSTRY
LAL LPNHE+ IRFU
Strategy for module construction
Si Wafer
Flip Chip
Module

## Slide 26: Infrastructures to contribute as an ATLAS production center Clean room (LAL, LPNHE, CEA-IRFU)

## Slide 27: Modern and state of the art for Pixel development: Captinnov plateform
High precision technology equipment for silicon devices characaterization & low noise electronics front end readout
Machine semi-automatic for probing devices
Integrated Fraday Cage for low current detection
Performances in terms of low courants (0.1 fA) et capacités (A.Farads)
Machine completely programmable
Possibilité of probe card insertion (Test multi-variables)
Ultra sonic wire bond machine , programmable with pattern recognition.
Probe station
Wire bondiong machine 20 mm
Semi automatic Karl Suss prober

## Slide 28: Cosmic and source for Pixel module testing
Digital scan
Analog scan
Analogue tests
Digital tests
Noise and dispersion
measurements
Tests of modules before and after irradiation
ATLAS Pixel Readout
Trigger by Wave-catcher
scintillator
scintillator

## Slide 29: Construction of a Laser testbench
29
Trigger
Optical fiber
From Module
Laser
Bias HV
To USBPix
USBPix system: ATLAS Standard device
Scan des pixels , dead pixel detection, cross talk.

## Slide 30
Pixel detector
Laser holder
Mechanics for inclined
pixel position
Improvement of Laser testbench
for pixel module Characterization
(PhD project- D. Hohov)
Under progress

## Slide 31: Captinnov Infrastructure
CAPTINNOV Clean Room
Man at Work
Probe station
Pixel under tests
Pixel Matrix

## Slide 32: Conclusions

## Slide 33: Comments & conclusions
An IN2P3 task force has been set to gather their efforts to contribute in a significant way to the construction of the new tracker for ATLAS phase 2
The ATLAS Phase 2 project is highly challenging requiring high level of technical expertise, for mastering precision silicon detectors, low noise electronics and many other aspects (mechanics, cooling, metrology…)
LPNHE and LAL are key players in ATLAS project since a long time, in various fields from Technology Computed Aided simulation, pixel sensor design, high precision low noise silicon characterization, to module assembly
Important technical infrastructures and skills have been accumulated
it offers an excellent opportunity for students to embark in one of the most attractive project for students and young scientist so Welcome!!

## Slide 34
Thank you for your attention and
welcome on board !!
LAL clean room
LPNHE clean room

## Slide 35: Improving efficiency: biasing solutions
CiS FE-I4 planar sensor, with four bias rail designs on the same sensor.
Both show increased noise for one design
Test beams:
A sample was tested in the CERN SPS test beam in July 2015.
  Reconstruction and data analysis performed at LAL.
  This device will be irradiated and tested in a future test beam.
Aim is to find a solution that reduces the inefficiencies in the biasing region within the pixel cell.
Testbeam: LAL & LPNHE joint activity

## Slide 36: The FBK/LPNHE Active Edge pixel 1 production
2013 4”n-on-p active edge production, on 200 µm FZ wafers
  Plus: 500 µm support wafer
Tested with radioactive source
And now on beam
4.5 μm wide
200 μm deep trench
M. Bomben et al. Nucl. Instrum. Meth. A 712 (2013) 41
9 FEI4-compatible sensors (IBL)
FBK-AE1

## Slide 37: Temporary metal at FBK
trench
Temporary metal
Technical solution allowing to remove the
metal grid used to bias pixels during tests.
After the metal removal, no inefficiency
left due to bias network
after resist patterning
Before temporary metal removal
After temporary metal removal

## Slide 38: DESY March testbeam
The sample: LPNHE5, featuring 100 µm pixel-to-trench distance and no GRs
  2 samples more available; not enough time to measure them
Several configurations tested
Results – next slides
beam
Testbeam: LAL & LPNHE joint activity

## Slide 39: CONCLUSIONS AND OUTLOOK

## Slide 40: Comments & Conclusions
The HL-LHC phase preparation is moving forward
The new tracker demands new (pixel) readout chip, cooling, mechanics, trigger, and sensors
The ATLAS IN2P3 R&D groups are involved in many of these activities playing a leading role in most of them
The LAL and LPNHE are important actors in this field thanks to new pixel productions, simulation studies, modules assembly, characterization and measurement

## Slide 41: BACKUP

## Slide 42: Tracker sensor design requirements
Thin : Low material Budget
Full geometrical sensitivity-Granularity
Radiation tolerant
Cost effective
Fast High Bandwith
Fast & High Bandwith
Low Material budget : Thin sensors
Full Sensitivity : Egless Sensors
Granularity 50x450  50x250 50x50 mm2
Radiation : use N-in-P and low thickness
Cost : N-in-N actual to N-in-P technology

## Slide 43: Breakdown voltage performance
Depletion Voltage: 20 V
Large breakdown voltage values already with 100 µm pixel-to-edge distance!
P-spray dose: 3x1012/cm2

## Slide 44: Pushing the limits
Chips/Modules
Edges width
Sensor Thickness
Sensor pitch
ASIC +sensor thickness
ASIC technology
Bump bonding technologies
2 CHIPs
1 CHIP
4 CHIPS
2010
1 mm
250 mm
100 mm  0
50X400
50X250
50x125
300 um
280 um
150um 75um, 50um
50x50
mms
mms
1 mm
500 um 150 um
0,25 um
0,13 um
0,065 um
0,040 um
Direct Bonding
~5 um
Bump bonding
~ 50 um
Micro Bump bonding
~ 10-20 um
SLID, TSV
~ 10 um
2013
2015-2017
202X
3D Technology
MICRON,ADVACAM ,VTT,
IZM ,EMFT,TEZZARON,CIS,
HAMAMATSU,TSMC,IBM, LETI

## Slide 45: Testing the the performances at the borders to increase the overall surface efficiency
Performances of pixels planaires under High energy Pions
bords
20030
(> 90% efficiency)
Last pixel column
(250 um)
Pixel border
Sensor border
Active Edge 50 mm
DUT#20
DUT#21
16 mm
17 mm
Distribution of residuals
Résultats presented at CERN
Atlas Upgrade Week-27-31/03/2017
D. Hohov, LAL
AIDA HIGH RESOLUTION PIXEL TELESCOPE

## Slide 46: In-pixel efficiency
No biasing structure (small) very uniform charge efficiency
  effect due to charge sharing at the pixel’s corners
Thr 1600, Vbias = -40 V